# Bend Loss on Optical Fibres

# Comparison of Results of OptiBPM, OptiFiber, and published reference 3

Sample problem is as in Reference 3, Table 1.  Original samples made 2004-11-16   on OptiBPM Ver 6.2, OptiFiber Ver 1.5

Associated Files

FibreBend1.bpd

FibreBend3.bpd

FibreBend4.bpd

FibreBendLoss.fcd

FibreBendLoss.doc

Bend Radius R = 300a = 0.5643 mm

Predicted Loss

Marcuse …   2a = 2.17 x 10-3  (  = 5.77 x 10-4 /m

OptiFiber …     Loss = 6.956 x 106  dB/km  (   = 8.00 x 10-4 /m  (Sakai & Kimura)

Loss = 8.65   x 106  dB/km  (   = 9.96 x 10-4 /m  (Snyder & Love)

In OptiBPM, use formula on the Relative Power vs. Distance data to obtain loss coefficient:

OptiBPM, FibreBend1.bpa   …  = 9.92 x 10-4  /m

OptiBPM, FibreBend4.bpa   …  = 9.17 x 10-4  /m

Bend Radius R = 500a = .94047 mm

Predicted Loss

Marcuse …   2a = 2.43 x 10-4  (  = 6.46 x 10-5 /m

OptiFiber …     Loss = 4.977 x 105  dB/km  (   = 5.73 x 10-5 /m  (Sakai & Kimura)

Loss = 5.880 x 105  dB/km  (   = 6.77 x 10-5 /m  (Snyder & Love)

OptiBPM, FibreBend3.bpa   …  = 8.23 x 10-5  /m

Reference

- J. Sakai, and T. Kimura, “Bending loss of propagation modes in arbitrary-index profile 
      optical fibers”, Applied Optics vol. 17,  no. 10, pp 1499-1506, May 1978

- W. Snyder and J. D. Love, "Optical Waveguide Theory," Chapman and Hall, 1983

- Dietrich Marcuse "Field deformation and loss caused by curvature of optical fibres"  J. Optical Society of America Vol. 66 No. 4 p 311 - 320 (1976)  Table 1.